## Slide 1
Mehmet Zor
Dokuz Eylul University
mehmet.zor@deu.edu.tr
Web: mehmetzor.com
General Information
About Composite Materials
Professor of Mechanical Engineering
İzmir - Turkey

## Slide 2: Contents
What is Composite Material?
Basic Properties of Composite Materials
Application Areas of Composites
Sample Products Containing Composites
Composites and Engineering Activities
Why Composite Material?
History of Composite Materials
Classification of Composite Materials
Disadvantages of Composites
Matrix Materials
Fiber Materials
Manufacturing Technologies in Composites

## Slide 3: 1-What is Composite Material?
A new material created by combining at least two different materials at the macro level (in such a way that they do not dissolve in each other) is called composite material.
The aim is to develop and bring together some features (lightness, strength, flexibility, etc.) that are not available in the components alone.

## Slide 4: 2- Basic Properties of Composite Materials
Although composite actually means mixture, it does not consist of soluble and dissolving components.
There is no exchange of atoms between the components.
Composite components do not chemically affect each other.
If the materials dissolve in each other and there is a mixture at the atomic level, such materials are not composites but alloys.
If the mixture is at the level of nanometer particles, these types of composites are called nano composites.

## Slide 5: 2-Basic Properties of Composite Materials
Composites are generally created from a main material called "matrix" and a more durable material called "reinforcement element (fiber)".
Of these two groups of materials, the reinforcement material increases the strength and load-bearing ability of the composite material.
The matrix material plays a role in preventing crack propagation that may occur during the transition to plastic deformation and delays the rupture of the composite material.
matrix
reinforcement element (fiber)
(continue)

## Slide 6: 3-Application Areas of Composites

## Slide 7: 3-Application Areas of Composites
With the developments in composite material technology, composites have begun to be used at increasing rates in industrial and technology applications.
Scientific studies on composites, which are used significantly especially in the aircraft industry and many other sectors, continue intensively today.
(continue)

## Slide 8: 3-Application Areas of Composites
Composite materials are used in a wide variety of areas thanks to their structure and properties. Since each sector has different needs and expectations, the product flexibility of composite materials appears as an important advantage.
Composites are used as raw materials in different sectors as well as as auxiliary equipment in manufacturing.
(continue)
The main sectors where composite materials are widely used and the product types used in these sectors are briefly summarized below:

## Slide 9: 3-Application Areas of Composites
Composites are used in many areas such as
(continue)
Space technology,
Maritime industry,
Manufacture of medical devices,
robotics technology,
chemical industry,
Electrical-Electronic technology,
musical instruments industry,
Construction and building industry,
Automotive industry,Defense
Industry and Aviation Sector,
Food and Agriculture Sector
Manufacturing of sports equipment (high jump poles, tennis rackets, surfing, racing boats, skis, etc.)

## Slide 10: 3-Application Areas of Composites
3.1 Buliding Sector:
Exterior and interior coverings
Decorative applications
Roofing sheets and roof detail profiles
Carrier profiles
Rainwater transport systems
Various purpose insulation Works
Concrete molds
Prefabricated buildings
Bridges
Water tanks, gratings, underground pipes, food aisle coverings. Observatory Domes, Open Field Cabinets, Bulletin Boards, etc.
(continue)

## Slide 11: 3-Application Areas of Composites
Window cores made of glass reinforced Polyester (GRP)
(continue)
3.1 Buliding Sector - (continue):

## Slide 12: 3-Application Areas of Composites
Prefabricated Buildings
(continue)
3.1 Buliding Sector - (continue):

## Slide 13: 3-Application Areas of Composites
Concrete columns are created by combining iron and concrete and are actually a composite structure.
iron bar (fiber)
Concrete (matrix)
(continue)
3.1 Buliding Sector - (continue):

## Slide 14: 3-Application Areas of Composites
Cabins
Piping
(continue)
3.1 Buliding Sector - (continue):

## Slide 15: 3-Application Areas of Composites
3.2 Automotive and Transportation Sector:
Automobile companies produce light automobiles in order to meet the needs of their customers and increase their competitiveness. Lightweight automobiles are very important in terms of mechanical (acceleration and braking) as well as energy saving.
(continue)

## Slide 16: 3-Application Areas of Composites
Automobile bodies,
Truck and bus side panels,
Truck trailer side slats,
Truck spoilers and front panels,
Container manufacturing,
Highway signs,Highway side pillars etc...
3.2 Automotive and Transportation Sector -(continue):
(continue)

## Slide 17: 3-Application Areas of Composites
Windshield Wiper; 30% Glass+PBT,
Filter Box; Mercedes, 35% Glass+Polyamide 66,
Pedals; 40% Glass+Polyamide 6,
Rearview Mirror; 30% Glass+ABS,
Headlight Body; BMW, 30% Glass+PBT,
Air Intake Manifold; BMW, Ford, Mercedes, 30% Glass+Polyamide 6,
Automobile Instrument Panel; CTP, GMT
Automobile Spoiler; CTP
Automobile Side Body Skeleton; Ford, CTP
Automobile body; Corvette, SMC GRP
GM car dashboard
Container manufacturing
(continue)
3.2 Automotive and Transportation Sector -(continue):

## Slide 18: 3-Application Areas of Composites
3.3 Defense Industry Applications:
Aircraft and helicopter body parts,
Aircraft nose and wing parts,
Mortar bodies and chests,
Bulletproof panel manufacturing,helmets,
Mine and assault boat parts and hulls,Shelters etc...
(continue)

## Slide 19: 3-Application Areas of Composites
3.4 Aviation Industry Applications :
Carbon composite sheet
Carbon honeycomb structure
Glass fiber
Aluminium
Steel & Titanium
(continue)

## Slide 20: 3-Application Areas of Composites
(continue)
3.4 Aviation Industry Applications (continue):

## Slide 21: 3-Application Areas of Composites
3.5 Food and Agriculture Sector Applications
Silos
Food storage tanks
Brine tanks
Aquaculture equipment
Greenhouses
Grain warehouses
Irrigation channels etc...
(continue)

## Slide 22: 3-Application Areas of Composites
3.6 Maritime Industry Applications:
Sailing/motor boats,
lifeboats,
buoys,
canoes,
Pontoons-piers,
marinemotorcycle,
Surfboard,
Marina equipment etc...
(continue)

## Slide 23: 3-Application Areas of Composites
3.7 Chemical Industry Applications:
Pipes and fittings for various purposes,
Chemical plant floor grids,
Acid tanks and coatings,
Anodized and galvano tanks,
Purification equipment,
Industrial platforms and railings,
Absorber and Scrubber (gas washing columns),
Ventilation ducts etc...
(continue)

## Slide 24: 3-Application Areas of Composites
3.8 Energy Sector Applications:
insulators,
antennas,
circuit breakers,
Fuse-panel boxes,
lighting bodies,
insulated platforms,
Electricity and lighting poles,
circuit breaker boxes,
Cable carriers,
cable channels,
Ladders, ballasts, etc.
(continue)

## Slide 25
4- Sample Products Containing Composites

## Slide 26
4-Sample Products Containing Composites
(continue)

## Slide 27
4-Sample Products Containing Composites
(continue)

## Slide 28: 5- Composites and Engineering Activities
As can be seen, composite materials can be used in many different sectors, they are constantly being developed and their usage rate is increasing day by day.
The probability of encountering composites in any business is quite high.
R&D activities for composite materials are frequently carried out not only in composite producing companies, but also in other companies depending on the usage situation.
In these activities, solutions and development alternatives with composite materials are possible.
For this reason, it is an important privilege and reason for preference for engineers to be able to carry out activities such as design, analysis, theoretical calculations, experimental measurements, developments and manufacturing for composite materials that they can do for isotropic (metal, ceramic, etc.) materials. This is only possible with a good basic knowledge of composite material mechanics.

## Slide 29: 5- Composites and Engineering Activities
The fact that the mechanical behavior of composites is different from isotropic materials and can vary depending on the direction requires that they be examined with different mechanical approaches and criteria.
Sir, let's make the shaft material composite. Let's look at von-mises stresses again.
If we make the shaft composite, it would be more accurate to evaluate it according to the Tsai-Hill criterion, not Von-Mises. Yield-fracture criteria for composites are different.
(continue)

## Slide 30: 6- Why Composite Material?
There is more than one answer to this question.
Composite materials, which have many advantages over other materials with their characteristic features, are preferred due to their many superior properties such as long life, lightness, high chemical and mechanical resistance.

## Slide 31: 6- Why Composite Material?
-Strength -Electrical conductivity
-Fatigue strength -Acoustic conductivity
-Wear resistance -Rigidity
-Corrosion resistance –Lightness
-Fracture toughness –Economy
-Thermal properties -Aesthetics
-Thermal conductivity
(continue)
The production of composite materials aims to improve one or more of the following properties:

## Slide 32: 6- Why Composite Material?
Materials | Density ρ (gr/cm3) | Tensile Strength σç (MPa) | Modulus of Elasticiy GPa | Specific Tensile Strength σç / ρ | Specific Modulus of Elasticity E/ρ
Non – Alloy Steel | 7.9 | 459 | 203 | 58 | 26
Alüminium | 2.8 | 84 | 71 | 30 | 25
Aluminium Alloy -2024 | 2.8 | 247 | 69 | 88 | 25
Brass | 8.5 | 320 | 97 | 38 | 11
Wooden (Beech) | 0.7 | 110 | 13 | 157 | 19
Bone | 1.8 | 138 | 26 | 75 | 14
Boron epoxy | 1.8 | 1600 | 224 | 889 | 124
Carbon-Epoxy-1 | 1.6 | 1260 | 218 | 788 | 136
Carbon-Epoxy-2 | 1.5 | 1650 | 140 | 1100 | 93
Kevlar-Epoxy | 1.4 | 1400 | 77 | 1000 | 55
S Glass-Epoxy | 1.8 | 1400 | 56 | 824 | 33
E Glass-Epoxy | 1.8 | 1150 | 42 | 639 | 23
When the material properties in the table below are examined, it is seen that composite structures are both much lighter and much more durable than classical metals.
(continue)

## Slide 33: 6- Why Composite Material?
6.1 High Specific Strength (strength/density ratio)
Composites with much higher strength values than those of classical metallic materials can be produced. Since their density is lower, the specific strength of the composites will be higher. For example: Composite profiles with high mechanical properties can be produced and used in constructions.
(continue)

## Slide 34: 6- Why Composite Material?
6.2 High stiffness/density ratio (Specific Rigidity):
(continue)
Composites with high stiffness/density ratios can be produced, which provides a significant advantage over classical materials.

## Slide 35: 6- Why Composite Material?
6.3 Lightness: Plastic-based composites are both lighter and have higher strength values than traditional materials. A profile section produced from composite material weighs approximately 1/4 of an equivalent steel profile.
(continue)

## Slide 36: 6- Why Composite Material?
The high electrical insulation properties of composites make them preferred in the manufacturing of many machine elements.They are also widely used in the electrical and electronics industry.Example: They are widely used in the production of elements such as transformers, cables and plates.
6.4 High Dielectric Resistance:
(continue)

## Slide 37: 6- Why Composite Material?
The anticorrosive properties of composites against environmental conditions are far superior to other materials.
Thanks to their high chemical resistance ability, composite materials are widely used in chemical plants and other areas at risk of chemical corrosion.
They are used in many areas, from chemical storage tanks to platforms and walkways.
6.5 Corrosion Resistance:
(continue)

## Slide 38: 6- Why Composite Material?
6.6 Diversity: Composite materials with different combinations with different mechanical properties can be manufactured.
(continue)

## Slide 39: 6- Why Composite Material?
Complex machine elements consisting of multiple parts can be manufactured as a single piece using composites.
In this way, since the number of parts will decrease, the production time is shortened as the interconnecting details and parts decrease.
However, it is very difficult to achieve this situation in traditional materials such as aluminum and steel.
6.7- Ease of Molding:
(continue)

## Slide 40: 6- Why Composite Material?
The polyester resin used in composites can be colored with special pigment additives and produced as self-colored according to the purpose.
6.8. Color variety:
(continue)

## Slide 41: 6- Why Composite Material?
Even complex machine elements can be easily designed with composite materials.
(continue)
6.9 Ease of design:

## Slide 42: 6- Why Composite Material?
Composites can be as light-permeable as glass.
Due to their transparency, they are used in greenhouses and solar collector manufacturing where light transmittance is important.
This multi-colored solar powered dome can be fitted with varied colored transparent composite material.
6.10 Transparency Feature:
(continue)

## Slide 43: 6- Why Composite Material?
Since concrete is porous, good adhesion is achieved due to the infiltration of polyester, one of the main components of the composite, into the pores of the concrete.
6.11 Applicability to concrete surfaces:
GRP polyester roof insulation
(continue)

## Slide 44: 6- Why Composite Material?
Composites are used as protectors and coatings on wooden surfaces. However, if the wood is dry, good adhesion must be achieved by adding polyester resin.
6.12 Applicability to wooden surfaces:
(continue)

## Slide 45: 6- Why Composite Material?
After cleaning the rust and oil residues on the metal surface, it can be coated with composites.
In this way, iron and steel surfaces can be protected from corrosion.
6.13 Applicability to metal surfaces
(continue)

## Slide 46: 6- Why Composite Material?
Flame resistance of composites depends on the properties of the polyester used.
Depending on the properties of the composite components, their resistance to burning can be increased.
Since their heat conduction is low, they are used as insulation materials.
Flame resistance can be improved with chemical additives.
6.14 Fireproof Feature:
(continue)
Composite materials, which have flame retardant, non-spreading and self-extinguishing properties, have a minimum level of toxic gas released during a fire.
With these features, they are used at critical safety points such as fire escapes.

## Slide 47: 6- Why Composite Material?
In particular, polyester resin-based composites from the thermoset plastic group do not change shape by softening. Thermal resistance depends on the type of polyester resin used.
6.15 Thermal Resistance :
ALUMİNE FIRE APPROACH AND ENTRANCE DRESS
Glass fiber, KEVLAR:
It is produced by coating a high temperature resistant aluminized polyester film on one side of the PBI / KEVLAR or Preox fabric under vacuum. Due to this special manufacturing technique, it does not crack or break, and is resistant to acid, base, salt and petroleum products. It protects firefighters by reflecting back 95% of the heat reflected from a 1000˚C heat source, depending on the type of fabric..
(continue)

## Slide 48: 6- Why Composite Material?
6.16 Repairability:
Composites can be repaired if damaged. A mold is used in the repair process. After the repair, sanding and painting are done.
(continue)

## Slide 49: 6- Why Composite Material?
6.17 Processability:
Composites are easily cut, drilled and sanded. Better results can be obtained if the tools used for this purpose are hard steel or diamond tipped.
(continue)

## Slide 50: 6- Why Composite Material?
6.18 Wide color and pattern options,
6.19 Flexibility,
6.20 Sealing (water insulation),
6.21 U.V. resistance to rays,
6.22 Ease of assembly
(continue)

## Slide 51: 7- History of Composite Materials
Since ancient times, human beings have tried to eliminate the fragility of fragile materials by putting plant or animal fibers into them.
The best example in this regard is adobe.
Fibers such as handle, straw and ivy branches added to the clay mud in adobe production increase the strength of adobe.

## Slide 52: 7- History of Composite Materials
Arrow bows made by stacking wooden boards with different properties and fiber directions on top of each other can be given as another example.
(continue)

## Slide 53: 7- History of Composite Materials
There are patents taken in the early 19th century about the production method of artificial stone slabs using hydraulic binders and fiber materials.
Cement and asbestos composites, which were first used to make thin sheets, have been used for years and are still used today.
(continue)

## Slide 54: 7- History of Composite Materials
On the other hand, it is understood from research that the application of fibers, which are widely used in reinforcing composites today, is not very new. For example, the production of glass fibers dates back to ancient Egypt.
Moreover, various items made of glass fibers of different colors from the XVIII Dynasty indicate that the manufacture of fine glass fibers was made in Ancient Egypt around 1600 BC.
(continue)

## Slide 55: 7- History of Composite Materials
The first record of the use of glass fibers in industry is dated 1877.
Synthetic resins reinforced with fibers have been used in industry since the 1950s.
The most well-known group of this material is "glass fiber reinforced polyester (GRP)".
(continue)

## Slide 56: 7- History of Composite Materials
These materials, known as "fiber-glass" in our country (Turkiye), have been used in the manufacture of elements such as liquid tanks, roof sheets, and small-sized sea boats since the 1960s.
The bodywork of "Anadol", the first mass-produced domestic car in Turkiye, is also made of this material.
(continue)

## Slide 57: 7- History of Composite Materials
Today, many different composite materials and products have been developed in many sectors such as aviation, shipping and energy.
(continue)

## Slide 58: 7- History of Composite Materials
Some promotional videos about composite materials:
http://wwwhttps://www.youtube.com/watch?v=0
https://www.youtube.com/watch?v=04K0bLwCDdM
https://www.youtube.com/watch?v=n3bWw8A2xwI
(continue)

## Slide 59
8- Classification of Composite Materials
The options for creating composite materials are almost endless. Therefore, they are very difficult to classify. However, common classifications will be emphasized here.

## Slide 60
8.1 According to Matrix Material Type:
8- Classification of Composite Materials

## Slide 61
(8.1 According to Matrix Material Type)
8.1.1 Metal Matrix Composites (MMC):
These materials are composites in which the main structure consists of matrix metal and a ceramic reinforcement phase is generally used as the reinforcement element.
There are almost no limitations in the choice of these materials.
8- Classification of Composite Materials
When looking at experimental studies, it is evident that many different species are used.A lot of research has been done on MMCs in the last 45-50 years and their properties have been mentioned positively in the literature.

## Slide 62
Metal matrix composites are the biggest alternative to traditional materials.
By combining the high elastic modulus of ceramics with the plastic deformation properties of metals, materials that are resistant to wear, have high fracture toughness and compressive stress are obtained.
These composites are widely used in the automotive, aerospace and defense industries.
8- Classification of Composite Materials
8.1.1 Metal Matrix Composites (MMC): (continue)
(8.1 According to Matrix Material Type)

## Slide 63
Ceramic materials are very hard and brittle.
They also have high temperature resistance and relatively low density properties.
Ceramics are materials with low thermal shock resistance and toughness. As examples of these; Al2O3, SiC, Si3N4, B4C, cBN, TiC, TiB, TiN and AIN can be given.
8.1.2 Ceramic matrix composites (CMC):
These compounds have different structures and ceramic matrix composites are obtained by using one or more of them depending on the purpose. Sandwich armor, manufacturing of various military parts and spacecraft are the main uses of these products.
8- Classification of Composite Materials
(8.1 According to Matrix Material Type)

## Slide 64
Carbon, ceramic and glass fibers added to the ceramic matrix are developed especially for special conditions such as high temperature applications.
If ceramic materials are reinforced with ceramic fibers, composites with higher strength and toughness values are obtained.
Recent studies on alumina and zirconia-based ceramic composites have led to the use of these materials as biomaterials in the human body.
8.1.2 Ceramic matrix composites (CMC) -continue:
8- Classification of Composite Materials
(8.1 According to Matrix Material Type)

## Slide 65
The most commonly used methods in the production of PMCs are hand lay-up, wet filament winding, moulding, pultrusion method, injection molding, extrusion methods.
PMCs are widely used in marine applications due to their corrosion resistance, in the automotive industry, other transportation industries and sports equipment manufacturing due to their lightness, and in automotive interior decorations due to their fireproof properties.
8.1.3 Polimer matrix composites (PMC):
8- Classification of Composite Materials
(8.1 According to Matrix Material Type)

## Slide 66
PMCs are widely used in marine applications due to their corrosion resistance, in the automotive industry, other transportation industries and sports equipment manufacturing due to their lightness, and in automotive interior decorations due to their fireproof properties.
8- Classification of Composite Materials
8.1.3 Polimer matrix composites (PMC) -continue:
The most commonly used methods in the production of PMC s are hand lay-up, wet filament winding, moulding, pultrusion method, injection molding, extrusion methods.
(8.1 According to Matrix Material Type)

## Slide 67
8.2 Classification According to Components Pair Alternatives
Matrix Materials | Reinforcement Elements | Shape of Composite Structure
Polymers | Fibers | Layers
Metals | Granular | Coatings
Ceramics | Whiskers | Film-Foil
 | Powder | Honey-Combs
 | Chip | Filament Wrapped Structures
  Granular: Grain-shaped raw material, rice-sized raw product obtained from recycling plastic bags.
  Whiskers: Chopped or ground fiber
8- Classification of Composite Materials

## Slide 68
8.3 Classification According to Shape and Placement of Reinforcement Elements :
Monolayer Composites b. Particulate Composites
c. Layered Composites d. Mixed (Hybrid) Composites
8- Classification of Composite Materials

## Slide 69
(8.3 According to Shape or Placement of Reinforcement Elements):
This type of composite consists of a single layer obtained by placing continuous or discontinuous fibers into the matrix structure.
The placement of the fibers is an important factor affecting the strength of the composite structure.
A fiber reinforced composite sheet consists of matrix and reinforcement/fiber components. These components do not dissolve or mix with each other.
8- Classification of Composite Materials
8.3.1 Fiber reinforced monolayer composites:

## Slide 70
By placing long continuous fibers parallel to each other (unidirectional) in the matrix, high strength is achieved in the direction of the fibers, but lower strength is obtained in the direction perpendicular to the fibers.
In composites with continuous fiber reinforcement (cross ply or woven fabric) placed in two directions perpendicular to each other, equal strength is provided in both directions.
8- Classification of Composite Materials
It is possible to create an isotropic structure at the macro level with short cut-discontinuous fibers distributed homogeneously in the matrix structure.
8.3.1 Fiber reinforced monolayer composites - continue:
unidirectional
Cross ply
Discontinous fiber
(8.3 According to Shape or Placement of Reinforcement Elements)

## Slide 71
8- Classification of Composite Materials
(8.3 According to Shape or Placement of Reinforcement Elements)
8.3.2 Particle Reinforced Composites:
If the particles are at the nanometer level, these types of composites are called nanocomposites.
Structures containing ceramic particles in a metal matrix have higher hardness and temperature resistance and are preferred in the production of aircraft engine parts.
They are obtained by reinforcing a matrix material with a particle-shaped material.
They are isotropic structures at the macro level. In other words, they show the same material behavior in all directions.
Particle and matrix do not dissolve into each other (macrolink).
The most common type is metal particles embedded in a plastic matrix.
The strength of the structure is directly proportional to the strength of the particles.

## Slide 72
8.3.3 Laminated (Layered) Composites
Composite layers (lamina) are obtained by placing more durable rod or woven fiber (rod or woven) materials into the matrix material.
Then, multiple layers are bonded on top of each other and a laminated composite plate is obtained.
In these layered structures, the orientation angle (q) of the fibers may differ from layer to layer.
8- Classification of Composite Materials
(8.3 According to Shape or Placement of Reinforcement Elements)
fiber
lamina
matrix
laminated
composites
plates
q: fiber orientation angle

## Slide 73
Laminated composite structures are the oldest and most widely used type of composites.
Very high strength values can be achieved by combining layers with different fiber orientations.
They are heat and moisture resistant structures.
They are lighter than metals and are preferred materials because they are more durable in the desired direction.
The orientation angle of the fibers is selected in directions where the stresses will be higher under operating conditions, and in this case, both lightness and strength are achieved at the same time.
Continuous fiber reinforced laminated composites are widely used as surface coating materials in aircraft structures, wings and tail groups.
8.3.3 Laminated Composites - Continue
8- Classification of Composite Materials
(8.3 According to Shape or Placement of Reinforcement Elements)

## Slide 74
Sandwich composite structures fall into the laminated composite material class. Sandwich structures are obtained by gluing higher strength plates to the upper and lower surfaces of a low-density core material that does not carry load and has only insulation properties.
8.3.3.1 Sandwich Composites
The bottom and top layers can each be an isotropic material or a fiber-reinforced layer.
8.3.3 Laminated Composites - Continue
8- Classification of Composite Materials
(8.3 According to Shape or Placement of Reinforcement Elements)

## Slide 75
8.3.3.1.1 Sandwich Composite Samples
Sandwich composite in honeycomb form
Sandwich composite panels used in exterior cladding
8.3.3 Laminated Composites
8- Classification of Composite Materials
(8.3 According to Shape or Placement of Reinforcement Elements)
8.3.3.1 Sandwich Composites-continue

## Slide 76
Different sandwich composite structures used in an aircraft fuselage
8.3.3.1.1 Sandwich Composite Samples
8.3.3 Laminated Composites
8- Classification of Composite Materials
(8.3 According to Shape or Placement of Reinforcement Elements)
8.3.3.1 Sandwich Composites-continue

## Slide 77
8.3.4 Hibrid Composites :
It is possible to have two or more fiber types in the same composite structure.
These types of composites are called hybrid composites.
This field is very suitable for the development of new types of composites.
For example, Kevlar is a cheap and tough fiber, but its compressive strength is low. Graphite is a fiber with low toughness, expensive but good compressive strength. The hybrid composite structure obtained by using these two fibers together has better toughness than graphite composite, lower cost and higher compressive strength than kevlar fiber composite.
8- Classification of Composite Materials
(8.3 According to Shape or Placement of Reinforcement Elements)

## Slide 78
Schematic Summary:
8- Classification of Composite Materials
(8.3 According to Shape or Placement of Reinforcement Elements)

## Slide 79
Samples
8- Classification of Composite Materials
(8.3 According to Shape or Placement of Reinforcement Elements)

## Slide 80
Composite structure of the tree
Composite structure of bone
8.4.1 Natural Composites
8.4 Other Types of Classification :
Materials such as wood and bone are natural composite materials.
8- Classification of Composite Materials

## Slide 81: 9- Disadvantages of Composites
The properties of the manufactured composite may not always be ideal. The quality of the material depends on the quality of the production method, there is no standardized quality.
Since laminated composites are sensitive to interlayer shear stresses, delaminations (separation between layers) may occur.
Since some composites are brittle, they are easily damaged, and their repair may create new problems.
They need to be cleaned very well and dried hot before they can be repaired. Some drying techniques can take a long time and be difficult.

## Slide 82
As mentioned before, a composite structure consists of 2 different materials called "Matrix" and "Reinforcement Element".
The matrix can be called the main material that forms the composite, and the reinforcement element can be called the more durable material that strengthens the matrix.
We will now examine each component in more detail:
10- MATRIX MATERIALS

## Slide 83
To transmit the forces to the fiber(s) and ensure their uniform distribution,
To protect the fibers from the effects of the environment and impacts,
Increasing the toughness of the composite material,
Preventing the formation of cracks in composites or the progression of cracks.
The matrix is the main component of the two important components of the composite material and forms the body of the structure.
10.1 Major contributions of matrix to composite
10- MATRIX MATERIALS

## Slide 84
Plastic matrix materials (Polymers)
a- Thermosets
b- Thermoplastics
c- Elastomers
Metal matrix materials (such as Aluminum, titanium, magnesium, etc.)
High temperature matrices (Ceramics)
10.2 Main Matrix Material Types:
10- MATRIX MATERIALS

## Slide 85
Plastic comes from the Greek word "plastikos", which means "able to take the desired shape".
In their simplest definition, they are synthetic materials with a long chain structure, called polymers, which are formed by adding small molecules called monomers to each other.
10.2.1 Plastic Matrix Materials (Resins/Polymers)
10- MATRIX MATERIALS
10.2 Main Matrix Material Types

## Slide 86
10.2.1.1 General Properties of Plastics :
The process of adding small molecules called monomers to each other under the influence of temperature, pressure and many chemicals and forming long chains called polymers (plastic) is called polymerization.
At the end of the polymerization process, ethylene (monomer) turns into polyethylene (polymer), propylene turns into polypropylene, and styrene turns into polystyrene. Thus, polymers (plastics) are formed.
10.2.1 Plastic Matrix Materials (Resins/Polymers)-Continue
10- MATRIX MATERIALS
10.2 Main Matrix Material Types

## Slide 87
Polymers (plastics) are used in many areas due to their low production costs, easy shaping and ability to be produced according to purpose.
Since approximately 90% of composites are produced from polymer (plastic) based matrices, composite materials are also called reinforced plastics.
10.2.1.1 General Properties of Plastics - Continue
Polymer molecules consist of many chains. They can form joined or unjoined (thermoplastic) or three-dimensional cross-linked chains (thermoset).
A promotional video: http://www.youtube.com/watch?v=QxazXEjI0SU
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.1 Plastic Matrix Materials (Resins/Polymers)

## Slide 88
It is possible to obtain resin with certain properties by stopping the polymerization process at certain stages.
While polymerization products can be used directly, their properties such as flexibility, strength, heat resistance and ultra-violet resistance are increased with additives and these are used in the manufacture of different products.
The main source of plastics is the residues of oil refineries.
Approximately 5% of the total oil produced in the world is used for plastic production.
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.1.1 General Properties of Plastics - Continue
10.2.1 Plastic Matrix Materials (Resins/Polymers)

## Slide 89
10.2.1.a – Thermosets :
They are also known as thermosetting plastics. (They harden with heat)
They have a very rigid structure because they are connected three-dimensionally by covalent bonds.
Because they are hardened by cross-linking, they do not dissolve or melt when heated.
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
a- Thermosets
b- Thermoplastics
c- Elastomers
We divided plastic materials into 3 groups.
Now we will examine these groups one by one:
10.2.1 Plastic Matrix Materials (Resins/Polymers)

## Slide 90
Thermoset plastics, which are in liquid form, are obtained by connecting monomer molecules with lateral bonds as a result of chemical reactions.
Since the polymerization reaction that takes place during their production is not reversible, they cannot be softened by heating and therefore cannot be shaped.
Thermosetting plastics are not reusable like thermoplastics, but they can be re-processed.
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.1.a Thermosets - Continue
10.2.1 Plastic Matrix Materials (Resins/Polymers)

## Slide 91
They need to be stored in freezers to prevent them from hardening.
Their shelf life varies between 6 and 18 months, provided they are kept in the freezer.
When they are taken out of the freezer and left at room temperature for a while (1-4 weeks), they harden, lose their properties and cannot be shaped.
Thermosetting resins do not dissolve under chemical effects
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.1.a Thermosets - Continue
10.2.1 Plastic Matrix Materials (Resins/Polymers)

## Slide 92
Major Thermoset Materials:
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
Polyester,
Epoxy,
Phenolic,
Silicon,
Polyimide,
Polyurethane,
Cynate Esters
High Temperature Resins
10.2.1.a Thermosets - Continue
10.2.1 Plastic Matrix Materials (Resins/Polymers)

## Slide 93
10.2.1.a.1 POLYESTER THERMOSETS
The word Polyester, which is a compound word, consists of the words "poly" meaning "lots of" and "ester" meaning an organic salt. It can also be expressed as “lots of organic salts”
Glass reinforced Polyester (GRP) tanks
Polyesters consist of chains of ester molecules and are formed by the polymerization of terephthalic acid and ethylene glycol.
Polyester is the most widely used resin in GRP applications both in Turkiye and in the world.
Polyester resins have high mechanical and chemical resistance at temperatures below 100 OC.
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.1.a Thermosets - Continue
10.2.1 Plastic Matrix Materials (Resins/Polymers)

## Slide 94
In addition to being used in the painting and rubber industry, they are used as protection against corrosion in metals and against moisture in wooden materials.
Their use is quite common in maritime (ship frames) and construction industry (building panels).
In addition, fiber reinforced polyesters are widely used in the production of elements such as pipes, tanks and automotive body parts.
10.2.1.a.1.1 Some Areas of Use:
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.1.a.1 POLYESTER THERMOSETS
10.2.1.a Thermosets
10.2.1 Plastic Matrix Materials (Resins/Polymers)

## Slide 95
Since polyester has a low viscosity before hardening, it wets the glass fiber well and forms a good composite with the glass fiber.
It is easy to use and low cost.
Different properties can be obtained by changing the bond shape (formula) of polyester.
It is suitable for use from simple molding such as hand lay-up to the most advanced molding techniques.
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.1.a.1.2 Some Advantages :
10.2.1.a.1 POLYESTER THERMOSETS
10.2.1.a Thermosets
10.2.1 Plastic Matrix Materials (Resins/Polymers)

## Slide 96
A high rate of shrinkage (between 5…12%) occurs during hardening. This causes the fibers to buckle and break under compressive stress.
There is difficulty in obtaining a smooth surface.
They emit poisonous gas.
Their shelf life is short.
Their corrosion resistance is low in alkaline and basic environments.
They decompose by taking in water.
GRP manhole cover
10.2.1.a.1.3 Some Disadvantages:
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.1.a.1 POLYESTER THERMOSETS
10.2.1.a Thermosets
10.2.1 Plastic Matrix Materials (Resins/Polymers)

## Slide 97
10.2.1.a.2 Epoxy
It is an adhesive chemical resin from the thermoset group.
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
It is produced by polymerization of the epoxide group and its properties can be changed with different formulas.
Depending on the type of hardener used, the properties of the composite material vary.
10.2.1.a Thermosets
10.2.1 Plastic Matrix Materials (Resins/Polymers)

## Slide 98
10.2.1.a.2.1 Superior Features
Its resistance to water, acid, oil and chemicals is very good and does not lose its resistance over time.
Epoxies, which are generally two-component, change from liquid to solid after a certain period of time.
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
It has excellent mechanical durability. It can withstand temperatures up to 140ºC when wet and 220ºC when dry.
It creates surfaces that are resistant to friction and wear.
epoxy floor coating
Low shrinkage occurs during hardening.
It has a wide range of colors in decorative applications.
10.2.1.a.2 Epoxy
10.2.1.a Thermosets
10.2.1 Plastic Matrix Materials (Resins/Polymers)

## Slide 99
By adding aggregate, friction resistance is increased and a floor with high slip resistance can be obtained.
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.1.a.2.1 Superior Features –Continue :
It forms a good bond with many fibres. If used with glass and carbon fiber, a composite with excellent mechanical properties can be obtained. These composites are widely used in the aerospace and marine industry.
It is a chemical resin used as an adhesive. Epoxy filled into the crack for repair purposes eliminates the discontinuity caused by the crack and prevents stress concentrations by connecting the crack edges together.
10.2.1.a.2 Epoxy
10.2.1.a Thermosets
10.2.1 Plastic Matrix Materials (Resins/Polymers)
It is aesthetic, easy to clean and hygienic. It does not contain solvent.

## Slide 100
Their costs are high.
They are harmful to the skin.
The right mix is extremely important.
Hardening of epoxy takes place between 127-177 ºC and under a certain pressure in approximately 1 hour.
Epoxies, which generally have two components, turn from liquid to solid after a certain period of time, like other thermoset plastics, and reach final hardness within a week or two.
10.2.1.a.2.2 Disadvantages
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.1.a.2 Epoxy
10.2.1.a Thermosets
10.2.1 Plastic Matrix Materials (Resins/Polymers)

## Slide 101
10.2.1.a.2.3 Usage Areas:
Making buildings resistant to environmental impacts has always been one of the most important discussion and research topics in the construction industry.
Epoxy is a very good building material developed against adverse conditions such as wind, storm, wave, thermal changes, freezing-thaw, pollution, chemical effects in nature and mechanical, physical and chemical adverse conditions in industry.
It is used to protect the interior and exterior surfaces of all kinds of land and sea structures and to increase their aesthetics.
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.1.a.2 Epoxy
10.2.1.a Thermosets
10.2.1 Plastic Matrix Materials (Resins/Polymers)

## Slide 102
Epoxy is used in pipe coatings as a surface protective coating, in can coatings as a primer, and on floors as an anti-wear coating or decorative coating.
In the construction industry; It is used in filling cracks and cavities, placing steel reinforcement and as an adhesive in structural elements.
It is used as an adhesive to bond fresh concrete to old hardened concrete, as well as in the assembly of prefabricated concrete elements and in the repair of cracks and fractures..>>
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.1.a.2.3 Usage Areas -Continue:
10.2.1.a.2 Epoxy
10.2.1.a Thermosets
10.2.1 Plastic Matrix Materials (Resins/Polymers)

## Slide 103
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
in repairing and eliminating manufacturing defects in wooden materials,
in bonding wood, metal (such as steel, aluminum) and stone materials,
as high-strength floor and wall paint and in underwater manufacturing,
in electrical and electronic device manufacturing,
in automotive industry due to its chemical resistance, hardness and adhesion properties.
Epoxy is also used,
10.2.1.a.2.3 Usage Areas -Continue:
10.2.1.a.2 Epoxy
10.2.1.a Thermosets
10.2.1 Plastic Matrix Materials (Resins/Polymers)

## Slide 104
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
The depletion of oil reserves in the world and the environmental pollution caused by existing energy sources have made the use of alternative energy sources inevitable. Wind energy, which gained momentum with the first major oil crisis, is one of these alternative sources. While wind turbines with a maximum capacity of 25 kW could be manufactured with the technologies of the early 1970s, thanks to the developments in composite and electrical-electronic technologies, today machines with a power of 5000 kW can be produced more economically. The blades of these turbines can be produced from glass-carbon-epoxy composite materials up to 60 meters long.
10.2.1.a.2.3 Usage Areas -Continue:
10.2.1.a.2 Epoxy
10.2.1.a Thermosets
10.2.1 Plastic Matrix Materials (Resins/Polymers)

## Slide 105
10.2.1.a.3 Phenolic Resins:
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
Phenol-formaldehyde is a condensation product and is a resin with solid and liquid types.
They can be used continuously up to 300 ºC, or for short periods up to 1000 ºC if reinforced with asbestos fiber.
They have high viscosity.
There is a high risk of pores forming. Therefore, high molding pressures are required.
After hardening, heat treatment must be applied up to 250 ºC.
They are resistant to water and many acids. However, they are sensitive to alkalis.
The surface quality of brittle phenolic resins is low.
10.2.1.a Thermosets
10.2.1 Plastic Matrix Materials (Resins/Polymers)
(Condensation reaction: It is the formation of a new molecule by separating a small and polar molecule between two molecules, one of which is an organic molecule.)

## Slide 106
10.2.1.a.4 Silicon:
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
It is one of many synthetic polymers containing silicon, oxygen and various hydrocarbons.
Although its mechanical properties are low, it can operate continuously up to 250 ºC.
Their resistance to water, heat and corrosion is very good.
Their costs are high.
10.2.1.a Thermosets
10.2.1 Plastic Matrix Materials (Resins/Polymers)

## Slide 107
10.2.1.a.5 Polyimide Resins:
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
It is a high temperature resin.
They can be used at temperatures up to 127-316 ºC.
They are difficult to produce.
These are high cost resins.
10.2.1.a Thermosets
10.2.1 Plastic Matrix Materials (Resins/Polymers)

## Slide 108
10.2.1.a.6 Polyurethane/Urethane :
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
It is a polymer consisting of a chain of organic units joined by carbamate links. They are used in the manufacture of materials such as foams, high-performance adhesives, synthetic fibers, gaskets, carpet underlays, and hard plastics.
Flexible polyurethane foams are also known as polyurethane sponges and are used as comfort materials in beds and furniture. Non-flexible polyurethane foams are mostly used for heat and sound insulation.
Polyurethane Waterproofing and Floor Covering
Polyurethane foam
10.2.1.a Thermosets
10.2.1 Plastic Matrix Materials (Resins/Polymers)

## Slide 109
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
Polyurethanes were first discovered by German scientist Otto Bayer in 1937.
Polyurethane is the indispensable material of the automotive, sponge, shoes, transportation, cooling, insulation, furniture, textile, food, electronics, paint and healthcare industry due to its biocompatibility.
Otto Bayer (1902-1982) and the polyurethane foam cork he produced
Polyurethane fabric
covered seat
100% Polyurethane leather
jacket
10.2.1.a.6 Polyurethane/Urethane : -Continue
10.2.1.a Thermosets
10.2.1 Plastic Matrix Materials (Resins/Polymers)
Polyurethane products are often called urethane. However, it should not be confused with the special urethane substance also known as ethyl carbamate. Polyurethanes are not made from ethyl carbamate and do not contain it.

## Slide 110
10.2.1.a.7 Cyanate Ester
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
Cyanate esters, which are high-performance thermosetting resins, are often used in the aircraft and electronics industries.
They can be used up to 200ºC in wet condition. Main features:
high thermal stability,
excellent mechanical properties,
good radiation and flame resistance,
extremely low dielectric constant,
minimum gas output,
minimum water absorption capacity
Very good insulation
10.2.1.a Thermosets
10.2.1 Plastic Matrix Materials (Resins/Polymers)

## Slide 111
10.2.1.a.8 Properties of Some Thermoset Matrices
Property | Polyester | Epoxy | Polyimide
Densitiy (gr/cm3) | 1.1 - 1.4 | 1.1 - 1.2 | 1.43 - 1.9
Modulus of Elasticity (GPa) | 1.2 - 4 | 2 - 5 | 3.1 - 4.9
Shear Modulus (GPa) | 1 - 2 | 1.5 | -
Tensile Strength (MPa) | 45 - 95 | 55 - 120 | 70 - 110
Compression Strength (MPa) | 140 - 90 | - | 288
Poisson Ratio | 0.35 -0.36 | 0.25 – .39 | -
Total Elangation (%) | 2 - 6 | 1.5 – 8.5 | 1.5 - 3
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.1.a Thermosets
10.2.1 Plastic Matrix Materials (Resins/Polymers)

## Slide 112
10.2.1.a.9 Processing of Thermosets
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
Thermosetting polymers are prepared for molding by mixing cross-linkers, additives and fillers into a low molar mass prepolymer.
They are in viscous liquid or powder form before being molded. In some applications, powder resins are reshaped and stored in granules, pallets, tablets or similar geometries by compressing them.
Thermosets stored by adding hardeners and accelerators are prone to cross-linking reactions during storage.
Therefore, they must be shaped within a suitable period of time.
Storage time is approximately two years for phenolic resins, although it is several weeks for uninhibited alkyd resins and unsaturated polyesters.
10.2.1.a.10 Molding methods of thermosets
1- Compression molding 2-Injection molding
2- Transfer molding 4- Casting
10.2.1.a Thermosets
10.2.1 Plastic Matrix Materials (Resins/Polymers)

## Slide 113
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.1.b Thermoplastics
Thermoplastics, which are widely used in both the automotive industry and the aircraft industry, are also called thermosoftening resins.
10.2.1.b.1 General Properties:
Their specific heat is 2 times that of metals and 4 times that of ceramics, and their thermal conductivity is 3 times lower than metals.
Thermoplastics, which are mostly produced by injection and extrusion molding methods, are used in GMT (Glass Mat Reinforced Thermoplastics) production techniques..
Thermoplastics soften when heated and harden again when cooled. They have thermal expansion coefficients approximately 5 times that of metals.
Durable and very flexible thermoplastic elastomer hose
10.2.1 Plastic Matrix Materials (Resins/Polymers)

## Slide 114
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.1.b.2 Advantages:
As raw materials, they have a long shelf life (shelf life: the life it can last when put on the shelf)
They have recycling capabilities.
They have a high ductility rate (1-500%).
Thermoplastic products can be reshaped by heating after processing.
Thermoplastics, which are solid at room temperature, can be stored
without refrigeration.
Organic solvents are not needed for their hardening.
Due to their superior fracture toughness, their impact resistance is also high. Its electrical insulation properties are very good.
10.2.1.b Thermoplastics
10.2.1 Plastic Matrix Materials (Resins/Polymers)

## Slide 115
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.1.b.3 Disadvantages:
They have very low strength (especially tensile strength), low hardness and low rigidity.
They are difficult to use as a matrix and their costs are high.
They are difficult to process at room temperature.
Solvents are needed to shape some thermoplastics into desired shapes.
Thermoplastic raw materials are more expensive than thermoset materials.
Creep (time-dependent deformation under constant load) may occur even at room temperature.
They have a low melting temperature.
10.2.1.b Thermoplastics
10.2.1 Plastic Matrix Materials (Resins/Polymers)

## Slide 116
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.1.b.4 Some Thermoplastic Materials:
Acetal/Poly-Methelene-Methylene (POM)
Polymet metha acrylic (Acrylic) (PMMA)
Acronitrile-Butadiene-Strain(ABS)
Poly-Tetra-Fluor-Ethylene (PTFE)
Poly-Amides (PA) / Nylon
Poly-Ethylene (PE)
Poly-Propylene (PP)
Poly-Vinyl-Chloride (PVC)
Poly-Ether-Sulphone (PES)
Poly-Ether-Imide (PEI)
Poly-Amide-Imide (PAI)
Poly-Phenylene-Sulfide (PPS)
Poly-Ether-Ether-Ketone (PEEK)
Poly-Styrene (PS)
10.2.1.b Thermoplastics
10.2.1 Plastic Matrix Materials (Resins/Polymers)

## Slide 117
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.1.b.4.1 Acetal/Poly-Methelene-Methylene (POM):
Its basic material is formaldehyde and is commercially known as Poly-Methelene-Methylene (POM).
It has high rigidity, strength, toughness and wear resistance.
Its melting point is (180oC) and its moisture absorption capacity is low.
With these properties, it is close to zinc and brass.
It is used in the manufacturing of elements such as some automobile parts, door handles, pump parts.
A fastener made of acetal
10.2.1.b Thermoplastics
10.2.1 Plastic Matrix Materials (Resins/Polymers)
10.2.1.b.4 Some Thermoplastic Materials:

## Slide 118
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.1.b.4.2 Polymet metha acrylic (Acrylic) (PMMA):
Acrylic or Poly-Met-Metha-Acrylic (PMMA) is amorphous because it is a linear polymer.
Due to its transparency, it is used as an alternative to glass in optical applications. (Ex: auto tail light lenses and aircraft windows)
Their low scratch resistance is a disadvantage compared to glass.
It is widely used in textiles and Poly-Acro-Nitrile (PAN) production.
Akrilik ip
Akrilik kazak
10.2.1.b Thermoplastics
10.2.1 Plastic Matrix Materials (Resins/Polymers)
10.2.1.b.4 Some Thermoplastic Materials:

## Slide 119
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.1.b.4.3 Acronitrile-Butadiene-Strain(ABS):
ABS, which has superior features, is two-phase.
1st phase: hard Strein-Acrylonitrile copolymer,
2nd phase: Strein-Butadiene copolymer and rubber.
It is obtained by mixing three different basic raw materials in different proportions.
A tool bag made of ABS
10.2.1.b Thermoplastics
10.2.1 Plastic Matrix Materials (Resins/Polymers)
10.2.1.b.4 Some Thermoplastic Materials:

## Slide 120
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.1.b.4.4 Poli-Tetra-Fluor-Ethylene (PTFE)
This material, also known as Teflon, has very good resistance to environmental and chemical effects.
It is not affected by water and has good electrical and thermal resistance.
It is used in the manufacturing of parts that cannot be lubricated due to low friction resistance.
It is also used in the chemical industry and food industry.
10.2.1.b Thermoplastics
10.2.1 Plastic Matrix Materials (Resins/Polymers)
10.2.1.b.4 Some Thermoplastic Materials:

## Slide 121
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.1.b.4.5 Poli-Amids (PA)
The most important PA family is Nylon (Nylon 6 and Nylon 6.6) and its strength, elasticity modulus and wear resistance are better than its equivalents.
It has a self-lubricating feature. It can maintain its mechanical properties up to 125oC.
Water absorption is its most important disadvantage.
It can be used instead of metal in places where low friction is required and high strength is not required (such as gears, bearings).
The second group is PA Aramids and their trade name is Kevlar. The specific strength of Kevlar is considerably higher than steel.
Door pull handles made of PA
10.2.1.b Thermoplastics
10.2.1 Plastic Matrix Materials (Resins/Polymers)
10.2.1.b.4 Some Thermoplastic Materials:

## Slide 122
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.1.b.4.6 Poly-Ethylene (PE)
PE, which has two types: low and high density, also has high deformation resistance.
They are used in film and wire manufacturing due to their superior properties such as low moisture absorption, low cost, chemical stability, easy processability and insulation.
High density PE has higher strength and rigidity. It is used in the manufacture of elements such as bottles and pipes.
PE pipes
Granulated PE
10.2.1.b Thermoplastics
10.2.1 Plastic Matrix Materials (Resins/Polymers)
10.2.1.b.4 Some Thermoplastic Materials:

## Slide 123
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.1.b.4.7 Poly-Propylene (PP)
It is a lightweight plastic used in injection molds and has a high specific strength value.
10.2.1.b.4.8 Poly-Vinyl-Chloride (PVC)
It is used in certain areas due to its high melting temperature.
They are used in food packaging, toys, flooring, windows
and doors manufacturing.
2. It is also used in areas such as rigid pipes, wire and cable insulation, and film manufacturing. PVC is unstable to heat and light.
10.2.1.b Thermoplastics
10.2.1 Plastic Matrix Materials (Resins/Polymers)
10.2.1.b.4 Some Thermoplastic Materials:

## Slide 124
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.1.b.5 Melting and Processing Temperatures of Thermoplastic Resins
Materials | Melting temperature range(°C) | Maximum process temperature (°C)
Poly-Propylene (PP) | 160-190 | 110
Poly-Amides (PA) | 220-270 | 170
Poly-Ether-Sulphone (PES) | - | 180
Poly-Ether-Imide (PEI) | - | 170
Poly-Amide-Imide (PAI) | - | 230
Poly-Phenylene-Sulfide (PPS) | 290-340 | 240
Poly-Ether-Ether-Ketone(PEEK) | 390 | 250
10.2.1.b Thermoplastics
10.2.1 Plastic Matrix Materials (Resins/Polymers)

## Slide 125
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.1.b.6 Mechanical and Thermal Properties of Thermoplastic Resins
Malzeme Adı | Specific Mass g/cm3 | Tensile Strength MPa | Modulus of Elasticity MPa | Temperature Limit oC
Poly-Ethylene (PE) (low density) | 0.92-0.93 | 7-17 | 105-280 | 80
Poly-Ethylene (PE) (high density) | 0.95-0.96 | 20-37 | 420-1260 | 100
Poly-Vinyl-Chloride (PVC) | 1.50-1.58 | 40-60 | 2800-4200 | 110
Poly-Propylene (PP) | 0.90-0.91 | 50-70 | 1120-1500 | 105
Poly-Styrene (PS) | 1.08-1.10 | 35-68 | 2660-3150 | 85
Acronitrile-Butadiene-Strain(ABS) | 1.05-1.07 | 42-50 | - | 75
Poly-Meth-Metha-Archylic (PMMA) | 1.11-1.20 | 50-90 | 2450-3150 | 125
Poly-Tetra-Fluorine-Ethylene(PTFE)(Teflon) | 2.10-2.30 | 17-28 | 420-560 | 120
Polyamide (PA) Nylon 6.6 | 1.06-1.15 | 60-100 | 2000-3500 | 82
10.2.1.b Thermoplastics
10.2.1 Plastic Matrix Materials (Resins/Polymers)

## Slide 126
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.1.c Elastomers
Elastomers, like thermosets, consist of long chains of molecules that are cross-linked. Under the influence of small forces, very large elastic deformations occur.
Elastic deformation of around 500% may occur in some elastomers.
Elastomer Buffer
10.2.1 Plastic Matrix Materials (Resins/Polymers)
The most important elastomer is rubber and can be divided into two categor
a- Natural rubber: obtained from certain plants.
b- Synthetic rubber:
They are used in thermoset and thermoplastic polymers and are produced through similar polymerization processes.

## Slide 127
10.2.2 Metal Matrix Materials:
Metal matrix composites are used in some fields such as automotive, space and aviation.
Since metal matrix materials have higher strength, rigidity and toughness than plastic matrices, they contribute greatly to the increase of these properties of the composite material.
Metals are used as matrix, albeit rarely.
10.2.2.1 General Features:
10- MATRIX MATERIALS
10.2 Main Matrix Material Types

## Slide 128
Since metal matrices do not form a good interface with every fiber, composite production is difficult and expensive, and this is one of their most important disadvantages. However, a good composite structure can be obtained with boron fiber whose surface is coated with silicon carbide.
Light metals such as aluminum, magnesium, nickel, titanium, copper, zinc and their alloys are frequently used metal matrix materials in composite production.
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.2 Metal Matrix Materials:
10.2.2.1 General Features -Continue:

## Slide 129
10.2.2.2 Aluminum and its Alloys
Examples of commonly used metal matrices are 6061 and 2024 aluminum alloys and 1010 pure aluminum.
Composite material is produced by hot pressing at 450-550 oC. Such a material retains its properties up to 300 oC.
Composites can be produced using Aluminum alloys and Carbon fiber. However, to prevent corrosion between them, the fiber surface is coated with nickel or silver.
They are preferred in areas where electrical conductivity is required.
In aluminum alloys, Mg, Mn, Si, Cu, and Zn alloying elements are used singly or several of them together and the desired properties are achieved.
Non-hardening Aluminium alloys: Al-Mg and Al-Mn,
Precipitation hardening Aluminium alloys: Al-Cu-Mg, Al-Mg-Si and Al-Zn-Mg
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.2 Metal Matrix Materials:

## Slide 130
10.2.2.3 Magnesium and its Alloys
Although the strength of Magnesium is lower than Aluminum, its specific strength is higher than Aluminium, since its density (1.74 g/cm3) is low.
Their disadvantages are that they have poor corrosion resistance, low rigidity and fatigue strength, and poor high-temperature creep and wear properties.
The alloying elements used with Magnesium are Aluminum and Zinc.
There are hardenable and non-hardenable types of magnesium.
It is better in machining than other metals.
Therefore, it is used in space and transportation vehicles and high-speed machines.
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.2 Metal Matrix Materials:

## Slide 131
10.2.2.3 Zinc and Its Alloys
The low melting temperatures of zinc (Zn) and its alloys (419oC) make them preferred as casting materials. Therefore, thin-walled, mixed-shaped and small-diameter holes with a thickness of 0.5 mm can be easily created.
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
Zn alloys produced by die casting are called Zamak: There are Zamak-3, Zamak-5, Zamak-8, Zamak-15 and Zamak-27 alloy types. These alloys are also coded as Z33520, Z35540 etc.
It provides corrosion resistance when coated on cast iron and steel, including Zn anode and steel/cast cathode (Zn coated steel = Galvanized steel).
The density of zinc is (7.13 g/cm3), which is a very high value.
Their wear resistance is very good at low speeds and heavy loads.
Zn and its alloys have good fatigue strength at room temperature.
They show a brittle character at low temperatures. While their ductility increases during long-term use, their strength decreases slightly.
10.2.2 Metal Matrix Materials:

## Slide 132
10.2.2.3 Titanium ve Its Alloysı
Titanium has one of the lowest coefficients of thermal expansion among metals. Additionally, its strength and rigidity are higher than Aluminium. Their corrosion resistance is also better than other metals.
Due to their heat resistance, titanium alloys are used in the manufacture of machine elements such as compressor fans and discs.
A fastener developed for the Boeing 787. Titanium Metal Matrix Composite (TMMC)
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.2 Metal Matrix Materials:
Composites can be produced by combining titanium alloys with Borsic and SiC (Silicon Carbide) fibers as matrix.
Their usage temperatures are around 420-550oC.It is used especially in the aircraft and space industry due to its superior specific strength.
The alloying elements used with titanium are Aluminum (Al), Manganese (Mn), Silicon (Si) and Vanadium (V).

## Slide 133
10.2.3 High Temperature Matrices
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.3.1 Ceramics
Ceramic, in its simplest definition, means "clay fired at very high temperatures". The history of ceramics is as old as the history of civilization.
Ceramic, with a more technical definition, is an inorganic compound obtained as a result of the combination and sintering of one or more metals with non-metallic elements.
Multifunctional, ceramic matrix composite/foam core sandwich construction.

## Slide 134
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.3.1.1 General Porperties:
Ceramics consist of silicates, aluminates, water and metal oxides, and alkali and alkaline earth compounds.
Oxides, nitrides, borides, carbides, silicates and sulfides are included in the ceramic group.
Some ceramics contain ionic and partially covalent bonds. Therefore, they have a very stable structure.
Some ceramics are amorphous, some are crystalline.
An F-16 Fighting Falcon F100 engine exhaust nozzle with five A500 Ceramic Matrix Composite gaskets.
(Gaskets are shown with yellow arrows.)
10.2.3 High Temperature Matrices
10.2.3.1 Ceramics
Ceramic materials are used in many areas such as industrial furnaces, electrical-electronics and optical industries.

## Slide 135
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
Although their strength is very high, ceramic materials have a very hard and brittle structure. Therefore, its usage areas are limited.
Melting temperatures are high (silica melts at 1750ºC, aluminate at 2050ºC). They are electrically and thermally insulating. If 6% aluminate is added to silica, the melting temperature drops to 1550ºC. Iron oxide and alkaline compounds can further reduce the melting temperature, down to 900ºC.
Turbine blade made of ceramic matrix composite
Since they have high thermal resistance, they are used in places exposed to high temperatures. Example: Industrial ovens, electronic and optical devices, etc.
10.2.3.1.1 General Porperties -Continue:
10.2.3 High Temperature Matrices
10.2.3.1 Ceramics

## Slide 136
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
Ceramic matrix composite materials can be used up to 1300oC. Example: SiC and Si3N4 ceramics reinforced with SiC (Silicon carbide) or Al2O3 (Alumina) fiber.
In such matrices (glass, ceramic, mullite, MgO, Al2O3, Sic), where carbon fiber is also used, the function of the fiber is to increase the toughness of the material.
A combustion chamber element made of ceramic matrix composite.
10.2.3.1.1 General Porperties -Continue:
10.2.3 High Temperature Matrices
10.2.3.1 Ceramics

## Slide 137
10- MATRIX MATERIALS
10.2 Main Matrix Material Types
10.2.3.2 Carbon Fiber – Carbon Matrix (Carbon/carbon)
Composites made of carbon matrix and carbon fiber can withstand up to 4000oC.
These composites have very good thermal and mechanical properties at high temperatures.
CMC (Ceramic Matrix Composites) coated carbon/carbon structures that reduce component weight.
10.2.3 High Temperature Matrices

## Slide 138: 11- FIBER MATERIALS
11.1 General Properties:
Fiber is the second main component of the composite and can be placed in the matrix in different shapes and arrangements.
Since there will be no need to place fibers in other directions, the composite structure is both lighter and more durable in the desired direction than classical metallic materials, and is more resistant to the same external loads, which is one of the most important purposes of composite manufacturing.
By placing continuous fibers, especially in directions where strength is important, the composite structure is provided with higher strength in those directions.

## Slide 139: 11- FIBER MATERIALS
11.2 Classification
Reinforcement materials can be examined in 3 categories:
Particle reinforcement elements,
Discontinuous fiber materials,
Continuous fiber materials
Now we will examine these categories one by one…>>

## Slide 140: 11- FIBER MATERIALS
Such reinforcing materials can be microscopic or macroscopic in size.
Particle reinforced composites can be considered as isotropic materials.
If the particles are at the nanometer level, these types of composites are called nanocomposites.
11.2.1 Particle reinforcement elements :
11.2.1.1 General Properties:
11.2 Classification

## Slide 141: 11- FIBER MATERIALS
They are used in the form of large and small particles
a. In composites where large particles are used, the load is carried by the components (matrix and fiber) together (e.g. aggregate).
b. Small particles increase the strength of the composite by preventing the movements of dislocations. Particle sizes do not exceed 1 μm (Ex: Al2O3 and SiC ceramics).
Aggregate
Lightweight Insulated Wall Block
Al2O3
(Alumina)
Alümina composite refractor panel
11.2.1 Particle reinforcement elements :
11.2.1.1 General Properties-continue:
11.2 Classification

## Slide 142: 11- FIBER MATERIALS
11.2.1.2 Advantages - Disadvantages :
The biggest disadvantage of particle reinforced composites produced by casting is the inability to wet the particles due to the decrease in melt viscosity and the difficulty in homogeneous distribution.
The production of particle-reinforced composites is more economical than fiber-reinforced composites.
However, fiber reinforced composites have superior mechanical properties than particle reinforced ones.
11.2.1 Particle reinforcement elements :
11.2 Classification

## Slide 143: 11- FIBER MATERIALS
11.2.2 Discontinuous Fibers (Chopped-Ground Fiber/Whiskers):
It consists of short cut fibers in the form of sawdust.
The diameters of the fibers do not exceed a few μm. Their lengths can vary from a few mm to a few cm.
Therefore, the fiber does not need to be very long to be defined as a fiber and not a particle.
11.2 Classification

## Slide 144: 11- FIBER MATERIALS
11.2.3 Continuous Fibers
Matrix
Continuous Fibers
The most important reinforcement materials used in composite structures today are continuous fibers. It consists of thin fibers placed throughout the matrix.
Continuous fibers play an especially important role in the development of modern composites.
In terms of the efficiency of the composite, fiber reinforcements are required to have the following properties:
1. Low density, 2. High modulus of elasticity, 3. High strength, 4. Hardness
Continuous fiber materials are produced and used in the form of rope without cutting, using methods such as wire winding.
11.2 Classification

## Slide 145: 11- FIBER MATERIALS
Reasons why fiber materials are high-performance engineering materials:
  Since they are produced on a small scale and the internal structure grain sizes are small, material defects are minimized. Therefore, they have superior microstructural properties. Therefore, their elasticity modulus and strength are high.
  Since the fiber length/diameter ratio is large, the amount of load transmitted to the fiber by the matrix also increases.
11.2.3 Continuous Fibers - Continue
11.2 Classification

## Slide 146: 11- FIBER MATERIALS
11.2.3.1 Woven Fabric Fibers
In order to obtain equal strength in different directions in a composite layer, fibers woven in the form of fabric are used.
There are types of woven fiber fabrics prepared with continuous fibers developed for different purposes.
11.2.3 Continuous Fibers - Continue
11.2 Classification

## Slide 147: 11- FIBER MATERIALS
11. 3 Major Fiber Materials :
Glass Fiber (or Fiberglass),
Carbon (Graphite) fiber,
Aramid (Kevlar) fiber,
Boron fiber,
Oxide fiber,
High density polyethylene fiber,
Polyamide fiber,
Polyester fiber,
Natural organic fibers
Among these fiber materials, Glass, Carbon, Boron and Aramid fibers are most commonly used. All three fiber types can be produced as continuous fibers.

## Slide 148: 11- FIBER MATERIALS
11.3.1 Glass fiber (or Fiberglass):
Glass fiber is produced from materials such as silica, colemanite, aluminum oxide and soda.
Glass fiber is the most commonly used fiber type in the production of fiber reinforced composites.
Glass fiber is produced by passing molten glass under pressure through a specially designed furnace with small holes at its base.
11. 3 Major Fiber Materials :

## Slide 149: 11- FIBER MATERIALS
After the glass fiber is shaped, a coating process is carried out to increase its resistance to wear.
Polymers that can be easily dissolved (with water) are generally used as fiber coating materials before composite production.
It is very important that the fiber and resin adhere well to each other. Otherwise, the hardness and strength of the composite material will be low. To prevent this situation, the fiber is coated with chemicals.
11.3.1 Glass fiber (or Fiberglass) - Continue:
11. 3 Major Fiber Materials :

## Slide 150: 11- FIBER MATERIALS
GRP PIPES
11.3.1 Glass fiber (or Fiberglass) - Continue:
11. 3 Major Fiber Materials :

## Slide 151: 11- FIBER MATERIALS
11.3.1.1 Glass fiber Types :
Glass A - It is the most commonly used glass type in windows and bottle manufacturing and is not used much in composite production.
11.3.1 Glass fiber (or Fiberglass) - Continue:
11. 3 Major Fiber Materials :
E Glass - It is the most commonly used type of glass in the production of reinforcement fibers. It has the features of low cost, good insulation and low water absorption rate.
S and R Glass - It is a high cost and high performance material. It is widely used in the aircraft industry. Since the diameters of the wires in the fiber are half of those of E Glass, the number of fibers increases. Therefore, the properties of the composite produced are very superior and a harder surface is obtained.
C Glass - It has high resistance to chemicals. It is used in places such as storage tanks.

## Slide 152: 11- FIBER MATERIALS
Carbon fiber, which was developed after 1965 and has found wide application especially in the aircraft and aerospace industry, is of great importance in composite technology.
Although glass fiber is the most commonly used reinforcement material today, carbon fiber is commonly used in advanced composite materials.
Carbon fiber is lighter and has better mechanical properties than glass fiber. However, its production costs are high.
It is used instead of metals in the skeletons of aircraft and sports vehicles.
Carbon fiber carbonizes when high heat treatment is applied. This new fiber is called graphite fiber. Today, carbon fiber and graphite fiber describe the same material.
11.3.2 Carbon Fiber:
11. 3 Major Fiber Materials :

## Slide 153: 11- FIBER MATERIALS
11.3.2 Carbon fiber -Continue:
11.3.2.1 Superior Properties of Carbon Fiber
High modulus of elasticity,
Low density,
High temperature resistance,
Corrosion resistance,
High hardness,
High strength and fatigue resistance,
Ability to create composites with all resins.
Disadvantage: It is expensive to produce.
11. 3 Major Fiber Materials :

## Slide 154: 11- FIBER MATERIALS
11.3.2.2 Carbon Fiber Types:
Continuous Carbon Fiber:
Available in Woven, Knitted and coiled. In tapes, prepregs, etc. is used.
Chopped Carbon Fiber (whichkers): They are generally used in injection molds, pressure vessels, machine elements manufacturing, and chemical environments.
11.3.2 Carbon fiber -Continue:
11. 3 Major Fiber Materials :

## Slide 155: 11- FIBER MATERIALS
11.3.2.3 Carbon Fiber Production Methods :
Carbon fiber is produced from two materials:
Pitch-based carbon fiber:
It is rarely used in structural applications because it has low mechanical properties.
Aircraft propeller made of carbon fiber
11.3.2 Carbon fiber -Continue:
11. 3 Major Fiber Materials :
PAN (PolyAcryloNitrile) based carbon fiber: It has high strength and is lighter. It is constantly being developed.

## Slide 156: 11- FIBER MATERIALS
11.3.3 Aramid Fiber (Kevlar)
In addition to being used as matrix, polymers are also used as fibers. Kevlar (Aramid) is a polymer fiber and a lightweight reinforcement material that provides high strength and rigidity to the composite structure. Aramid is aromatic polyamide, a type of nylon.
Aramid fiber is better known in the market under its trade names Kevlar (DuPont) and Twaron (Akzo Nobel). The most commonly used Kevlar (Aramid) fibers are Kevlar 29 and Kevlar 49.
Aramid fiber with different properties can be produced for different applications. Its natural color is usually yellow.
11. 3 Major Fiber Materials :

## Slide 157: 11- FIBER MATERIALS
11.3.3 Aramid Fiber (Kevlar) – Continue:
11.3.3.1 Some Outstanding Features:
Low density,
High strength and fatigue resistance,
High impact resistance and wear resistance,
High chemical resistance,
E-Compressive strength close to glass fiber,
Kevlar fiber composites are 35% lighter than glass fiber composites.
11. 3 Major Fiber Materials :

## Slide 158: 11- FIBER MATERIALS
11.3.3.2 Disadvantages:
Some types of aramid fibers are sensitive to ultraviolet rays.
Since they are sensitive to light, they need to be stored in the dark.
They may not bond well with the matrix. In this case, microscopic cracks may occur in the resin. These cracks can lead to water absorption when the material fatigues.
11.3.3 Aramid Fiber (Kevlar) – Continue:
11. 3 Major Fiber Materials :

## Slide 159: 11- FIBER MATERIALS
11.3.3.3 Some Areas of Use:
Ballistic protection applications; Military helmets. High impact resistant Kevlar 29 is used in the manufacture of bulletproof vests.,
Protective clothing; gloves, motorcycle protection clothing, hunting clothes and accessories.
3-Other Fields: Sail masts for sailing yachts, Body parts in aircraft, Boat hull,Belt and hose for industrial and automotive applications,Fiberoptic and electromechanical cables, Friction linings and brake drums in clutches, Gaskets, packing etc. used in high temperatures and pressures.
11.3.3 Aramid Fiber (Kevlar) – Continue:
11. 3 Major Fiber Materials :

## Slide 160: 11- FIBER MATERIALS
11.3.4 Boron Fiber:
The type of fiber that is stronger and also more expensive than carbon fiber is boron fiber.
Boron is the second lightest element that is solid at room temperature. It is manufactured by coating boron on a thin wire called the core (usually Tungsten/Wolfram). Therefore, boron fiber is a composite in itself.
11. 3 Major Fiber Materials :

## Slide 161: 11- FIBER MATERIALS
Boron-tungsten fibers are produced by passing hot tungsten streamer (thin wire) through H and Bortichloride (BCl3) gas. Thus, a boron layer forms on the outside of the Tungsten filament.
Boron fibers are produced in different diameters. It is used in aviation due to its high mechanical properties.
Its resistance to high temperatures is increased by coating with silicon carbide (SiC) or Boron Chloride (B4C). Especially with (B4C) coating, its tensile strength increases significantly.
Since the cost of boron fiber is high, carbon fiber has been used more in recent years.
11.3.4 Boron Fiber - Continue:
11. 3 Major Fiber Materials :

## Slide 162: 11- FIBER MATERIALS
11.3.5 Some Material Properties:
Properties | E-Glass | S-Glass | Boron | Carbon | Kevlar49
Density (gr/cm3) | 2.54 | 2.49 | 2.68 | 1.85 | 1.44
Tensile Strength.(MPa) | 2000 | 4750 | 3450 | 2900 | 3750
Modulus of Elasticity(GPa) | 80 | 89 | 414 | 525 | 136
Fiber Diameter (µm) | 3-200 | 3-13 | 100-1000 | 5-13 | 12
Coeff. of Thermal Exp. (1/oC) | 5x10-6 | 2.9x10-6 | 3xx10-6 | -1x10-6 | -2x10-6
Kopma Uz. (%) | 2.75 | - | 0.7 | 0.5-1.3 | 2.5
11. 3 Major Fiber Materials :

## Slide 163
11.3.6 Tensile Curves of Fiber Materials
11- FIBER MATERIALS
11. 3 Major Fiber Materials :

## Slide 164
12- Manufacturing Technologies in Composites
Manufacturing methods of the composite may vary depending on the reinforcement and matrix material, part shape, and the properties targeted from the composite.
Raw materials, mold, heat and pressure are generally needed to produce a part.
During manufacturing, care should be taken to ensure
that the fiber has an evenly spaced and homogeneous distribution,
that the fiber materials are thoroughly wetted by the matrix since they are sensitive to mechanical contact,
and that a strong interface is created between the fiber and the matrix.
12. 1 General Features of Manufacturing Methods:
In addition to the resin and reinforcement material used, the manufacturing method also plays an important role in determining the final properties of a composite structure.
Here, the most commonly used methods in the production of composites will be included. .>

## Slide 165
5. Grouping of Manufacturing Methods According to Composite Material Type:
12- Manufacturing Technologies in Composites
12. 1 General Features of Manufacturing Methods:
Manufacturing Methods
Thermoset Materials:
Thermoplastic Materials:
Short fiber Composites
Continius fiber Composites
Short fiber Composites
Continius fiber Composites
SMC molding
SRIM
BMC molding
Spray -Up
Injection molding
Flament Winding
Pultrusion
Resin Trans. Molding
Hand Lay-Up
Autoclave
SCRIMP,RIFT,VARTM..
Injection Molding
Blow Molding
Thermal Shaping
Tape Wrapping
Press Molding
Autoclave

## Slide 166
Hand Lay-Up
Spray-Up
Wet Filament Winding
Resin Transfer Molding (RTM)
Pultrusion
Compression molding
  Sheet Moulding Composites (SMC)
  Bulk Moulding Composites (BMC)
Vakum Bonding / Vakum Bagging
Autoclave bonding
6. Major Composite Manufacturing Methods are listed below :
Now we will examine these methods one by one..>>
12- Manufacturing Technologies in Composites
12. 1 General Features of Manufacturing Methods:

## Slide 167
12.2 Hand-Lay-up Method
In this manual manufacturing method,
the mold to be used is first cleaned and gel-coat is applied.
Then, the resin-impregnated fabrics are left to cook/dry under room temperature and atmospheric pressure or under different temperatures and pressures..
Layered composite materials can also be produced by stacking fibers in the form of layers.
12.2.1 General Features
Resins can be impregnated to fabrics in layers, or depending on the properties of the fabric, resin can be impregnated to multiple layers at the same time.
12- Manufacturing Technologies in Composites
After the gel-coat hardens, fiber fabrics are placed in this mold by hand, and at this time, resin is impregnated (is fed) with the fibers with a roller or brush.

## Slide 168
The most commonly used matrix materials in the hand-laying technique are polyester and epoxy, although vinyl-ester and phenolic resins are also preferred.
Although manual laying requires intensive labor, it is suitable for small quantities of production.
Application Areas: Wind turbine blades, plates, boat manufacturing, moldings,…
12.2.2 Advantages of the Method
It is very easy to learn and apply.
The cost is low, especially when using resins that bake at room temperature.
It is very easy to obtain materials suitable for the method.
Compared to spraying, higher fiber density and continuous long fibers can be used.
12.2.1 General Features - Continue
12- Manufacturing Technologies in Composites
12.2 Hand-Lay-up Method

## Slide 169
The method depends very much on the dexterity of the person performing the lamination (layering). It is very difficult to achieve high “Fiber Volumetric Density”.
12.2.3 Disadvantages of the Method
Video-1 : How To Hand Lay Up a Carbon Fibre Skateboard
The density and viscosity of the resins used in this method are low. In terms of human health, such resins are more harmful than heavy molecule resins.
Without quality ventilation systems, it is difficult to keep the Styrene concentration escaping into the air within legal limits for polyester and vinylester.
12- Manufacturing Technologies in Composites
12.2 Hand-Lay-up Method
If the resin ratio is kept low, a high percentage of air voids and non-wetting areas may occur.

## Slide 170
12.3 Spray – up Method
The spray method can be considered as an instrumental form of the hand lay-up method. The chopped fibers are sprayed onto the mold surface, together with resin containing hardener, by means of a special gun.
The trimming process of the fiber is done with an independently working trimmer located on the gun. After the spraying process, the surface is smoothed with a roller to prepare the product.
12- Manufacturing Technologies in Composites

## Slide 171
The mold surface is coated with a mold release agent.
Gel-coat is applied to the mold surface and waited for it to harden.
12.3.1 Process Steps:
Fibers are chopped (turned into short fibers) in a hand gun and production is carried out by spraying these fibers mixed with catalyst/hardener into a mold.
After a certain thickness is achieved, the material is generally left to cure under ambient conditions.
12- Manufacturing Technologies in Composites
12.3 Spray – up Method

## Slide 172
12.4 Wet Filament Winding Method
The fiber winding method consists of continuous fiber being wetted with resin and then pulled from a spool and wound on a rotating mold (mandrel).
By winding the continuous fiber into the mold at different angles, products with different mechanical properties can be obtained. This method is often used in the production of hollow parts such as pipes and tanks. After winding a sufficient number of fiber layers, the product hardens and is separated from the rotary mould.
12- Manufacturing Technologies in Composites

## Slide 173
The fibers wound on bobbins pass through a resin bath.
Resin impregnated fibers are wound in the desired orientation angle on the mandrel, which is rotated around its axis at a certain speed by a moving mechanism.
After reaching the desired thickness or number of layers, the process is completed.
The drying process is carried out at room temperature and in an oven.
12.4.1 The process steps of the method are briefly as follows.
12.4 Wet Filament Winding Method
12- Manufacturing Technologies in Composites

## Slide 174
12.4.2 Advantages of the Method:
Low labor,
Superior mechanical properties due to winding with different orientation angles,
Reproducibility.
12.4.3 Disadvantages of the Method:
High investment is required.
It can only be used in the manufacture of tubular products.
Surface quality is not high.
12.4 Wet Filament Winding Method
12- Manufacturing Technologies in Composites

## Slide 175
GRP Pipe Technology: Continuous Fiber Winding Process
Promotional videos of Wet Filament Winding Method :
Video 2
Video 3
12.4 Wet Filament Winding Method
12- Manufacturing Technologies in Composites

## Slide 176
12.5 Vacuum Asisted Resin Infusion Molding (VARIM)
This Method is used in the production of high quality, large composite parts. The process steps can be summarized as follows:
The mold surface is covered with a separator.
Dry fabrics (fiber) or a preform material are deposited into the mold in a certain arrangement.
Peeling fabric, release film and resin dispersing films are placed on the fabric.
Using a plastic vacuum nylon (film) and double-sided adhesive sealants, the stacked fabrics are isolated from the external environment all around.
With the help of vacuum, the resin is completely penetrated into the stacked dry fabrics and the material is left to cook.
Video 4
12- Manufacturing Technologies in Composites

## Slide 177
12.6 Resin Transfer Molding ( RTM )
Unlike the VARIM method, two molds (female and male) with gel coat applied are used here. Reinforcement materials specially produced for RTM are placed in the mold. The molds are closed. And resin is injected into the material under pressure.
In some applications, vacuuming is also done to help advance the resin. Generally, composite products with a wall thickness of 2-10 mm and a fiber content of 20-30% are obtained.
12- Manufacturing Technologies in Composites

## Slide 178
12.6.1 Main Features of the Method
RTM is faster than the hand lay-up method and the product has a longer life. However, it is necessary to use a two-piece mold.
The RTM method can be applied with or without gel-coat. It is a suitable method for products where both surfaces are required to be smooth.
Felt, fabric or a combination of the two is used as reinforcement material.
After the reinforcement material is placed in the mold, it is coated with resins that dissolve slowly in the matrix to prevent it from being dragged in the mold and the mold is closed.
12- Manufacturing Technologies in Composites
12.6 Resin Transfer Molding ( RTM )

## Slide 179
The resin is pumped into the mold under pressure. Matrix injection is applied cold, warm or heated up to 80ºC.
In this method, the resin must penetrate well into the fiber in order to remove the air and toxic gases inside and obtain a non-porous product. Vacuum can be used for this.
It may require long-term workmanship when placing the fiber into the mold. Complex parts can be produced with this method. For example; Some parts of Concorde planes and F1 cars are produced using this method.
12.6.1 Main Features of the Method - Continue
12- Manufacturing Technologies in Composites
12.6 Resin Transfer Molding ( RTM )

## Slide 180
The resin viscosity should be low enough to wet the fibers and seep between them.
There should be rapid hardening at high temperatures and minimal distortion during cooling.
It should come out of the mold easily.
Organic binders in reinforcement materials should not dissolve in the resin.
12.6.2 Points to Consider :
12.6.3 Some Application Areas:
Small, complex aircraft and automobile parts, train chairs or chairs, etc.
RTM Introduction video : Video 6
12- Manufacturing Technologies in Composites
12.6 Resin Transfer Molding ( RTM )

## Slide 181
12.6.4 Advantages of the Method:
Production speed is high.
The fiber/resin ratio and the amount of voids can be perfectly controlled.
Thus, products with high fiber content and low air gap can be obtained.
Dimension/tolerance adjustment of complex shaped parts is very good.
All parts are obtained with the same quality.
Since production is carried out in a closed environment, it is advantageous in terms of health and safety.
It requires less labor than some methods.Both surfaces of the material come out smooth.
Molds must be rigid enough to absorb the pressure. This increases cost and weight.
Production is generally limited to small parts. The cost is high and mold design is difficult.
There may remain parts where the resin has not penetrated, resulting in expensive waste.
12.6.5 Disadvantages of the Method:
12- Manufacturing Technologies in Composites
12.6 Resin Transfer Molding ( RTM )

## Slide 182
12.7 Pultrusion Method
In this method, resin-impregnated fibers are generally drawn through a mold and profile rods with various cross-sectional geometries are produced.
Molds are generally made of chrome-plated bright steel.
12.7.1 General Features
2. In the system, the continuous reinforcement material is passed through the resin bath and then passed through the forming mold heated to 120-150 ºC to obtain the product.
Due to the use of continuous fibers, very high mechanical properties are obtained in the reinforcement direction.
12- Manufacturing Technologies in Composites

## Slide 183
As the fibers are pulled at a constant speed in a heated mold, the composite part comes out of the mold cooked or partially baked.
With pultrusion, it is possible to produce parts with constant cross-section and continuous length.
These parts generally come out of Pultrusion without the need for additional surface treatment.
12.7.1 General Features –Continue:
12- Manufacturing Technologies in Composites
12.7 Pultrusion Method

## Slide 184
12.7.2 Advantages of the Method:
GRP profile pipes produced by pultrusion method
Pultrusion is a continuous and automatic process that allows for low-cost, fast production.
The resin ratio can be controlled accurately.
Fibers are more economical because they are used as thread.
Products consisting of smooth fibers and having high fiber volumetric ratios may have high structural performance.
12- Manufacturing Technologies in Composites
12.7 Pultrusion Method

## Slide 185
12.7.3 Disadvantages of the Method:
It is limited to the production of fixed cross-section parts only.
The use of heated molds is a cost-increasing factor.
They are used as beams and poles, in carrier systems, bridges, stairs, building cage systems and skeletons.
12.7.4 Application Areas
Pultrusion Introduction video :
Video 7
12- Manufacturing Technologies in Composites
12.7 Pultrusion Method

## Slide 186
12.8 Compression Molding
In this production technique, ready-made molding components (glass fiber, resin, additives and filling materials) are converted into products in hot press molds (SMC, BMC).It has advantages such as the production of complex elements, embedding metal parts within the body, and obtaining different wall thicknesses.
In addition, both sides of the product are shaped with a mold. Material consumption is low. Complex elements that cannot be produced with other composite production techniques can be produced with this method. Compression molding is usually applied in two ways (SMC, BMC):
12- Manufacturing Technologies in Composites

## Slide 187
12.8.1 SMC Technique
In the SMC (Sheet Molding Composites) technique, continuous fibers are cut into 25-50 mm lengths and combined with the matrix material (resin) in the form of a pulp.
Video 8 SMC
12- Manufacturing Technologies in Composites
12.8 Compression Molding
In the SMC (Sheet Molding Composites) technique, continuous fibers are cut into 25-50 mm lengths and combined with the matrix material (resin) in the form of a pulp.The fiber ratio in the total weight of the composite is approximately
25-30%. The sheets produced are generally 1 m wide and 3 mm thick.

## Slide 188
BMC (Bulk Molding Composites) is the name given to the dough-shaped material formed by pre-combining chopped fiber as a reinforcement material and a resin as a filling material, and the technique by which it is obtained.
This method is similar to RTM. The difference from RTM is that the resin/fiber mixture is made outside the mold and is melted and injected into the empty mold under pressure.
12.8.2 BMC Tecnique
Low viscosity thermoset resins are well suited for this method.It is faster than other methods. Many products, from children's toys to aircraft parts, can be produced using this method.
12- Manufacturing Technologies in Composites
12.8 Compression Molding

## Slide 189
12.9 Vacuum Bonding / Vacuum Bagging
After the composite material (usually large sandwich structures) is placed in a mold, a vacuum bag is laid and covered as the top layer.
By sucking the air inside, the vacuum bag is pulled down by applying 1 atm pressure on the deposited material.
In the next step, the entire composition is placed in an oven and heated to cure the resin.
This method is often applied in conjunction with fiber winding and laying techniques.
Vacuum bagging method is also used in composite material repair processes.
12- Manufacturing Technologies in Composites

## Slide 190
12- Manufacturing Technologies in Composites
12.9 Vacuum Bonding / Vacuum Bagging

## Slide 191
12.10 Autoclave
Autoclave is a pressurized vessel in which pressure, temperature and vacuum (suction) can be controlled. In order to increase the performance of thermoset composite materials, it is necessary to increase the fiber/resin ratio and completely eliminate air gaps that may occur in the material. This requires high heat and pressure, which is only possible in an autoclave device.
As in the vacuum bagging method, the fiber/resin is exposed to pressure in a sealed bag. This pressure must be greater than 1 atm, regular and controllable. Thus, high quality composites can be produced for special purposes and curing conditions are fully met. This method can take much longer and is more expensive than other methods.
12- Manufacturing Technologies in Composites